# Supplementary materials

|  | PBS | PHBV | Flax fibres | Makroblend |
| --- | --- | --- | --- | --- |
| Processing temperature | [160 – 180] °C | [160 – 175] °C |  | [260 – 270] °C |
| Mould temperature | 20°C | 60°C |  | 80°C |
| Drying | 50°C ¦ 9h | 50°C ¦ 9h | 50°C ¦ 9h | 105°C ¦ 3h |

Table S1 : Processing parameters of the materials studied.

Figure S1 : SEM pictures of fixed biofilmafter ageing.

A-B: PBS, S1-780. C: PHBV-Flax, S1-780. D: PHBV-Flax, S2-1740.

Figure S2 : SEM pictures of PBS after ageing.

A-B: S1-780. C-D: S2-1740.

Holes observed in picture B are very scarce on the overall surface.

Figure S3 : SEM pictures of PBS-Flax after ageing.

A-B: S1-780. C-D: S2-1740.

Figure S4 : SEM pictures of Makroblend after ageing.

A-B: Before ageing. C: S1-780. D: S2-1740.

|  |  | Strain at break % | Stress at break MPa | Young’s modulus MPa |
| --- | --- | --- | --- | --- |
| PHBV | Initial | 0.9 ± 0.1 | 32.2 ± 2.2 | 4422 ± 193 |
|  | S1-780 | 1.4 ± 0.1 ↗ 58 % | 34.7 ± 0.2 ↗ 7.8 % | 4292 ± 358 ↘ -2.9 % |
|  | S2-1740 | 1.5 ± 0.1 ↗ 73 % | 34.9 ± 0.6 ↗ 8.3 % | 3866 ± 321 ↘ -13 % |
|  | L1-Abio | 1.1 ± 0.1 ↗ 26 % | 37.5 ± 0.6 ↗ 17 % | 4410 ± 229 ≈ -0.3 % |
| PHBV Flax | Initial | 1.1 ± 0.4 | 26.8 ± 2.4 | 7259 ± 302 |
|  | S1-780 | 0.7 ± 0.0 ↘ -36 % | 15 ± 2.1 ↘ -44 % | 3240 ± 276 ↘ -55 % |
|  | S2-1740 | 1.0 ± 0.4 ↘ -7.3 % | 15.4 ± 1.9 ↘ -42 % | 3832 ± 277 ↘ -47 % |
|  | L1 | 2.0 ± 0.2 ↗ 77 % | 27.66 ± 0.6 ↗ 3.2 % | 4406 ± 418 ↘ -39 % |
| PBS | Initial | 136.4 ± 60.3 | 29.4 ± 1.3 | 633 ± 19 |
|  | S1-780 | 20.0 ± 0.4 ↘ -85 % | 36.0 ± 0.3 ↗ 23 % | 716 ± 50 ↗ 13 % |
|  | S2-1740 | 17.5 ± 2.6 ↘ 87 % | 36.1 ± 0.1 ↗ 23 % | 656 ± 48 ↗ 3.7 % |
| PBS Flax | Initial | 31.52 ± 0.3 | 3.9 ± 0.4 | 2700 ± 132 |
|  | S1-780 | 22.6 ± 1.1 ↘ -5.9 % | 3.7 ± 0.8 ↘ -28 % | 1873 ± 263 ↘ -31 % |
|  | S2-1740 | 17.4 ± 1.2 ↘ -31 % | 2.7 ± 0.3 ↘ -45 % | 1841 ± 117 ↘ -32 % |
| MkB | Initial | 47.5 ± 0.4 | 127 ± 2.6 | 2145 ± 81 |
|  | S1-780 | 48.1 ± 0.8 ↗ 1.2 % | 122.4 ± 3.3 ↘ -3.6 % | 1851 ± 89 ↘ -14 % |
|  | S2-1740 | 45.4 ± 4.3 ↘ -5% | 94.8 ± 47.5 ↘ -25 % | 1738 ± 155 ↘ -19 % |
|  | L1 | 47.4 ± 2.2 ≈ -0.35 % | 125.2 ± 8.5 ↘ -1.5 % | 1769 ± 182 ↘ -18 % |

Table S2 : Evolution of tensile properties after ageing for all the materials studied

Figure S5 : Tensile curves of the materials studied before and after ageing.

A-B: PBS at high and low deformation. C: PBS-Flax. D: MkB

Figure S6 : Tomography of PHBV samples before and after ageing.

(A) Initial (B) L1-Abio (C) S1-780 (D) S2-1740

|  |  | Tm (°C) | ΔHm (J.g-1) | χc (%) |
| --- | --- | --- | --- | --- |
| PHBV | Initial | 174.9 ± 0.1 | 81.8 ± 0.2 | 56.0 ± 0.1 |
|  | S1-780 | 171.9 ± 1.4 | 87.0 ± 2.1 | 59.6 ± 1.5 |
|  |  | ↘ -1.7 | ↗ 6.4 | ↗ 6.4 |
|  | S2-1740 | 173.1 ± 1.3 | 81.9 ± 1.3 | 56.1 ± 0.9 |
|  |  | ↘ -1.1 | ≈ 0.2 | ≈ 0.2 |
|  | L1-Abio | 174.6 ± 0.4 | 80.5 ± 1.3 | 55.2 ± 0.9 |
|  |  | ≈ -0.2 | ≈ -1.5 | ≈ -1.5 |
| PHBV-Flax | Initial | 173.8 ± 0.9 | 52.1 ± 2.6 | 51.0 ± 2.5 |
|  | S1-780 | 173.1 ± 2.9 | 58.0 ± 0.5 | 56.8 ± 0.5 |
|  |  | ≈ -0.5 | ↗ 11.4 | ↗ 11.4 |
|  | S2-1740 | 169.8 ± 0.4 | 56.2 ± 2.9 | 55.0 ± 2.8 |
|  |  | ↘ -2.4 | ≈ 7.9 | ≈ 7.9 |
|  | L1-Abio | 174.1 ± 0.2 | 59.2 ± 2.1 | 58.0 ± 2.1 |
|  |  | ↗ 0.1 | ↗ 13.6 | ↗ 13.6 |
| PBS | Initial | 116.9 ± 0.3 | 64.2 ± 0.8 | 32.1 ± 0.4 |
|  | S1-780 | 116.6 ± 0.2 | 69.2 ± 2.3 | 34.6 ± 1.2 |
|  |  | ≈ -0.2 | ↗ 7.68 | ↗ 7.68 |
|  | S2-1740 | 116.8 ± 0.2 | 69.8 ± 1.8 | 34.9 ± 0.9 |
|  |  | ≈ -0.1 | ↗ 8.72 | ↗ 8.72 |
| PBS-Flax | Initial | 116.7 ± 0.7 | 49.2 ± 2.5 | 35.1 ± 1.8 |
|  | S1-780 | 116.1 ± 0.0 | 50.4 ± 0.2 | 36.0 ± 0.2 |
|  |  | ≈ -0.5 | ≈ 2.45 | ≈ 2.45 |
|  | S2-1740 | 114.5 ± 0.2 | 62.9 ± 2.2 | 44.9 ± 1.6 |
|  |  | ↘ -1.9 | ↗ 28 | ↗ 28 |
| MkB | Initial | 225.3 ± 0.9 | 18.9 ± 1.6 | n.d. |
|  | S1-780 | 224.8 ± 0.2 | 20.6 ± 1.2 | n.d. |
|  |  | ≈ -0.2 | ≈ 9 | X |
|  | S2-1740 | 224.5 ± 0.6 | 21.8 ± 2.4 | n.d. |
|  |  | ↘ -0.4 | ↗ 15.4 | X |

Table S3 : thermal properties of the studied materials during the first scan

|  | Mw (103 g.mol-1) | Mn (103 g.mol-1) | Ip |
| --- | --- | --- | --- |
| Reference | 154 ± 33 | 23.9 ± 3.6 | 6.2 ± 0.5 |
| S2-1740 | 246 ± 37 | 27.6 ± 10 | 7.6 ± 1.3 |
| S1-780 | 184 | 22 | 8.3 |

Table S4 : Molecular weights measured by Gel Permeation Chromatography on PHBV-Flax specimens before and after aging